## Slide 1
Inspection and identification systems enabling the reuse and recycling of EoL composite materials
Miguel Gómez – AIMEN
Camilo Prieto - AIMEN
19th Feb 2025 (online)

## Slide 2: Content overview
5th webinar | 19-02-2025 | online
AIMEN Technology Centre
EURECOMP Project introduction
Inspection Technologies
Identification Technologies
Conclusions
  Hyperspectral Imaging
  Laser Induced Spectroscopy Analysis (LIBS)
  Raman Spectroscopy
  Active Thermography
  Ultrasound Testing

## Slide 3: AIMEN Technology Centre
5th webinar | 19-02-2025 | online
Innovation and Technology Centre that develops
R&D&i activities and provides technological services to the industry in the fields of:
MATERIALS, ADVANCED MANUFACTURING PROCESSES, DIGITIZATION and SUSTAINABILITY.
Non-profit private association: 300+ employees
9500m² of scientific-technological infrastructures
55+ years of experience (since 1967)
250+ R&D&i projects in last 10years
50 R&D projects per year

## Slide 4: Introduction: EURECOMP project
EU project with a strong focus on circularity, set out to provide sustainable methods towards repair, recycling and reuse of end-of-life composite materials
https://eurecomp.eu

## Slide 5: Inspection technologies
5th webinar | 19-02-2025 | online
Failure analysis of wind turbine blades and aircraft composite structures is critical for assessing potential reuse in other applications.
Identifying the root causes of damage enables evaluation of structural integrity and determination of suitable secondary uses.
This promotes safety, sustainability, and waste reduction by extending the lifecycle of composite materials.
COMMON DEFECTS
  Delamination:
  Layers of the matrix and fiber of the composite are separated.
  Blisters:
  Are small air pockets
  Inclusions of foreign material
    Cracks:
    Fissures, fractures and breaks

## Slide 6: Non-Destructive Testing (NDT)
5th webinar | 19-02-2025 | online
A group of methods used to evaluate the integrity, properties, or defects of materials or components without causing damage, using techniques like ultrasonic testing, radiography, and thermography, ensuring safety, quality, and reliability across industries.
THERMOGRAPHY
ULTRASOUND TESTING (UT)

## Slide 7: Test Specimen – case study
5th webinar | 19-02-2025 | online
50 x 50 cm Glass Fiber Reinforced Polymer piece with artificial defects.
Description:
  Made of 12 plies of glass-fiber filled with epoxy
  Thickness of 10 mm
  25 numbered half-way hole defects
  Defects are found at three different depths:
    2.5 mm
    5 mm
    7.5 mm

## Slide 8: Active Thermography
5th webinar | 19-02-2025 | online
It involves the use of a heat source to stimulate an object with a heat pulse. An infrared camera records a video of the object to measure the heating and cooling process on the object's surface.
FEATURES
  High speed analysis
  Provide two-dimensional thermal images
ISSUES
  Non-uniform surface heating
  Lateral heat difusion
  Environmental noise

## Slide 9: Active Thermography: Postprocessing Methods
5th webinar | 19-02-2025 | online
A thermal image sequence post-processing method that involves the calculation of the phase of a thermal image sequence using a Discrete Fourier Transform.
Pulsed Phase Thermography
Principal Components Thermography
A statistical technique used to identify specific patterns in large datasets containing a high number of features per observation and analyze them to enable the depicting of similarities and differences of specific patterns
PULSED PHASE THERMOGRAPHY
PRINCIPAL COMPONENT THERMOGRAPHY

## Slide 10: Laser Active Thermography
5th webinar | 19-02-2025 | online
Advantages
Homogeneous illumination
Adjustable beam shape and size
Modulable warming curve
Selective analysis area
Allow scanning procedure
Issues (current setup)
Smaller inspection area
Laser Beam 0-order
Laser
IR camera
Mirror
Specimen
Difractive optical element (DOE)
PC+SW acquisition and analysis

## Slide 11: Ultrasound Testing (UT)
5th webinar | 19-02-2025 | online
Based on the detection and the feature extraction of the ultrasonic waves reflected by defects. UT works by sending ultrasonic waves through an object or material. These high frequency sound waves are transmitted into materials to characterise the material or for flaw detecting.
  FEATURES
The depth of penetration for flaw detection is superior to other NDT methods
Sensitive to both surface and subsurface discontinuities
  ISSUES
Surface must be accessible to transmit ultrasound
It requires a coupling medium
A technical expert required to acquire and interpreted the data

## Slide 12: Ultrasound Testing: Pulse-Echo
5th webinar | 19-02-2025 | online
Ultrasound pulse-echo devices are built with a transducer which produces a wide-band pulse that is subjected to the test material during testing. The pulse travels through the material until it meets with either discontinuity within the material or when it reaches a new medium. The wave is then scattered or reflected back to the transducer.
  No defect: The echo passes through the part and returns to the receiver, showing only the input and output signals.
Porosity: Detected because noise appears between the input and output signals, but unlike a delamination, the signal is not lost as long as the porosity is not too high.
Delamination: Detected by the receiving signal. The output signal decreases considerably or even disappears if the delamination is large compared to the input signal.

## Slide 13: Ultrasound Testing: Representation
5th webinar | 19-02-2025 | online
A-Scan: radio-frequency waveform presentation showing the time and amplitude of an ultrasonic signal.
S-Scan: image that represents a cross-sectional view derived from a series of A-scans.
B-Scan: image showing a cross-sectional profile through one vertical slice of the test piece.
C-Scan: two-dimensional presentation of data displayed as a top view of a test piece.
Amplitude
Time
Time
Depth
Width
Depth
Time
Width

## Slide 14: Thermography and Ultrasound Testing Tool (TUTT)
5th webinar | 19-02-2025 | online
AIMEN developed its own software for working with Non-Destructive Testing methods
Application uploaded to EuReComp Zenodo: https://zenodo.org/records/13833956

## Slide 15: Identification technologies
5th webinar | 19-02-2025 | online
Chemical recycling of composites is a very active topic for fiber-reinforced polymer matrix: solvolysis
In-situ material identification is one the challenges for chemical recycling of End-of-Life composite waste utilizing solvolysis methods
OBJECTIVE: To develop innovative identification systems by means of spectroscopic techniques and advanced data processing algorithms:
Hyperspectral Imaging (HSI)
Laser Induced Breakdown Spectroscopy (LIBS)
Raman Spectroscopy
Chemometrics and machine learning

## Slide 16: Thermoset matrix samples
5th webinar | 19-02-2025 | online
 | Resin type | Hardener type
#1 | Epoxy | Aliphatic Polyamines
#2 | Epoxy | Aliphatic polyamine
#3 | Epoxy | Aliphatic Polyamines
#4 | Epoxy | Aromatic amine
#5 | Vinylester | Methyl ethyl ketone peroxide
#6 | Polyester | Methyl ethyl ketone peroxide
Epoxy
aromatic amine
Vinylester
Polyester
polyamine

## Slide 17: Hyperspectral imaging
1st EuReComp workshop, 2023/04/20, Dresden
  It combines the power of digital imaging and spectroscopy.
  Every pixel in the image provides local spectral information across a large number of spectral bands.
  spectral data  used to chemically identify the materials.
  spatial data  to get the spatial distribution of each material along the sample.
Intensity
Wavelength λ
5th webinar | 19-02-2025 | online

## Slide 18: Hyperspectral imaging
Multi&Hyperspectral Imaging Scanning Techniques
5th webinar | 19-02-2025 | online
5th webinar | 19-02-2025 | online

## Slide 19: Hyperspectral imaging
5th webinar | 19-02-2025 | online
400 – 1000 nm
2.1 nm resolution
300 spectral channels
900 spatial channels
Reflection & transmission
Reflection
InGaAs Sensor
Sample
Halogen
lamps
900-1700 nm
4.7 nm resolution
168 spectral channels
900 spatial channels
Silicon Sensor​

## Slide 20: Hyperspectral imaging
5th webinar | 19-02-2025 | online
Optical characterization in VIS and SWIR spectral ranges
SWIR
VIS
Red: 640 nm
Green: 550 nm
Blue: 460 nm
#1 #2
#3 #4
#5 #6
5th webinar | 19-02-2025 | online

## Slide 21: Hyperspectral imaging
5th webinar | 19-02-2025 | online
Optical characterization in VIS and SWIR spectral ranges
SWIR
SWIR
Red: 1660 nm
Green: 1155 nm
Blue: 980 nm
  From the reflectance spectra, distinctive spectral bands for the different materials can be identified. Those bands (feature selection) can be used for discrimination models
  Absorption peaks in #2, #3 at 1550nm

## Slide 22: Laser Induced Breakdown Spectroscopy (LIBS)
FEATURES:
  No sample preparation required
  Multiple element detection
  Qualitative and quantitative analysis
  In-situ and fast analysis
  Surface & depth-profiling technique
  Versatility (material types and forms)
Optical emission spectroscopic technique based on analysis of plasma generated during laser ablation -> provides information about chemical composition of sample
Sample elements emits specific wavelength
(public database available)
High power laser pulse ablation
High temperature plasma creation
Light emission as the plasma cools
Crater on sample ( ~mm)
Intensity
400 500 600
Emission spectrum
Wavelength (nm)
5th webinar | 19-02-2025 | online

## Slide 23: Laser Induced Breakdown Spectroscopy (LIBS)
5th webinar | 19-02-2025 | online
Excitation Laser
  (wavelength, pulse duration, pulse energy, rep. rate)
Focusing optics
  (focal length –> spot size)
Optical collection
  (magnification, spectral range)
Spectrometer and detector
  (spectral resolution, efficiency and time-resolved capabilities)
XYZ stage
  (precision, travel range)
Optical collection
Focussing optics
Laser
Field spectrometer(s)
Lab spectrograph
& iCCD
Sample
Automated XYZ stage
Echelle spectrometer
Lasers
Workstation PC for data acquisition and data analysis

## Slide 24: LIBS spectra measurement
5th webinar | 19-02-2025 | online
5th webinar | 19-02-2025 | online

## Slide 25: LIBS spectra on thermosets
To identify the emission lines
5th webinar | 19-02-2025 | online

## Slide 26: LIBS spectra on thermosets
5th webinar | 19-02-2025 | online
Atomic emission lines

## Slide 27: LIBS spectra on thermosets
Molecular emission lines
5th webinar | 19-02-2025 | online

## Slide 28: LIBS spectra on thermoset resins
5th webinar | 19-02-2025 | online

## Slide 29: Laser Induced Breakdown Spectroscopy (LIBS)
Experimental data
LIBS spectra
Normalization
Table of features
Feature selection and dimensionality reduction
Classification algorithms
MATRIX CLASIFICATION
5th webinar | 19-02-2025 | online

## Slide 30: Laser Induced Breakdown Spectroscopy (LIBS)
Experimental data
LIBS spectra
Normalization
Table of features
Feature selection and dimensionality reduction
Classification algorithms
MATRIX CLASIFICATION
5th webinar | 19-02-2025 | online

## Slide 31: Raman Spectroscopy
5th webinar | 19-02-2025 | online
Laser excitation in UV, VIS or NIR
UNDERLYING PRINCIPLE
Inelastic scattering of laser light by material surface: los (gain) to molecular and lattice vibrations
Excitation to and subsequent relaxation from virtual energetic levels
FEATURES
Detailed molecular structure information from vibrational modes. Material specific emission peaks
Non destructive technique
Comparably weak signal
Organic and inorganic materials.
Not affected by wáter interference, unlike IR spectroscopy.
Most common use is materials ID (fingerpint)

## Slide 32: Raman Spectroscopy
5th webinar | 19-02-2025 | online
Spectrometer
Sample
Laser
Beam splitter
Notch filter
Microscope
objective
Raman setup at Aimen
Raman microscope at Patras University
Main components and parameters
Laser excitation source
Peak wavelength & power
Optical collection system
  Probe geometry and type
Spectra detection
  Spectral range, resolution, Dark noise
Baseline and fluoroscence removal
Spectra - > Raman shift calculation

## Slide 33: Raman Spectroscopy
5th webinar | 19-02-2025 | online
Individual Raman peaks can be assigned to specific vibrational modes of the analysed molecule
Material-specific lines allow for its identification and differentiation from other materials

## Slide 34: Raman Spectroscopy
5th webinar | 19-02-2025 | online
Individual Raman peaks can be assigned to specific vibrational modes of the analysed molecule
Material-specific lines allow for its identification and differentiation from other materials

## Slide 35: Conclusions
5th webinar | 19-02-2025 | online
Technologies for enabling informed decisions for material circularity pathways
  Active Thermography
  Ultrasound Testing
  Hyperspectral Imaging
  Laser Induced Spectroscopy Analysis
  Raman Spectroscopy
Systems and experimental protocols coupled with machine learning algorithms enables differentiation of matrix of fiber-reinforced EoL composites -> Support recyclers on solvolysis optimization
The methods and software developed allow inspection of parts and detection of defects, as well as material changes -> Support decision whether to repair, reuse or recycle a component

## Slide 36
Miguel Gómez
Miguel.gomez@aimen.es
Camilo Prieto
Camilo.Prieto@aimen.es
AIMEN Technology Centre
5th webinar | 19-02-2025 | online